# Lab 2 — Instructor Key: Axial Deformation, Redundant Members and Thermal Stress

For instructors only. Do not distribute to students. Every number in this key is computed by src/lab02_analysis.py (and src/make_key.py) from sample_data.csv and src/specimen_measurements.json, or by the simulation’s own model code run in Node. To build a key for your own class data, put your CSV and measurements in the same format and run python3 src/lab02_analysis.py your.csv your_measurements.json, then python3 src/make_key.py. Uncertainties are expanded (U=2u) unless marked u. Sign convention as in the handout (Beer 8e): tension positive; P on the caps is a compressive magnitude.

## 1. Results at a glance (sample data)

Table K1. Results from the sample data.

| Quantity | Result | Reference / theory |
| --- | --- | --- |
| Part A area bt (mm²) | 161.29 (uA/A = 0.21 %) | 161.29 nominal |
| E of 6061-T6 (GPa) | 68.46 ± 0.93 | 68.9 ± 2.0 |
| ν | 0.330 ± 0.006 | 0.33 ± 0.02 |
| G=E/21+ν (GPa) | 25.74 ± 0.37 | about 26 |
| Bending fraction β; offset e | 0.0545 ; 0.0577 mm | — |
| E front gage only / back only (GPa) | 64.88 / 72.45 | — |
| Pgap (kN) | 6.951 ± 0.051 | Eq. 10 with height-gage g: 6.9 ± 2.8 |
| Gap g from the knee / height gage (mm) | 0.0401 ± 0.0012 / 0.040 ± 0.016 | true value 0.0400 |
| Share s after contact | 0.3712 ± 0.0073 | Eq. 12: 0.3689 ± 0.0076 |
| Tube force at 30 kN (kN) | −8.527 | Eq. 11: −8.561; no-gap formula: −11.070 |
| Rod / tube stress at 30 kN (MPa) | −169.5 / −38.4 | yield 370 / 276 |
| Cap compliance C (mm/kN), below / above knee | 1.99 ± 0.16 / 1.44 ± 0.04 (u) | true value 1.50 |
| dFb/dT (N/K) | 97.6 ± 9.9 | Eq. 16: 94.3 ± 6.9 |
| Preload at 20 °C (kN) | 1.998 | 2.0 set |
| Bolt / sleeve stress at 80 °C (MPa) | 100.0 / −34.5 | — |
| α of 6061-T6 inferred from Part C (10−6/K) | 24.02 ± 1.40 | 23.6 ± 0.6 |
| D1 acceptable fixed gap (mm) | 1.43 to 4.81 | — |

The sample data were generated from a known “truth” model (src/generate_sample_data.py, values in src/truth.json). It includes a 5.5 % bending fraction in Part A, a +0.6 % gage-factor error, a cap compliance and a seating toe in Part B, and a residual thermal output of +0.4 µε/K and a temperature-dependent sleeve modulus in Part C. The closure test in tests/test_lab02_independent.py confirms that the analysis recovers every truth value within its stated uncertainty.

## 2. Pre-lab solutions

P1. (a) A=25.40×6.35=161.29 mm²; σ=18 000/161.29=111.6 MPa, 40 % of the 276 MPa yield strength. εx=σ/E=1620 µε; εy=−νεx=−535 µε. A 1 µε resolution is 0.56 % of the axial strain at 2 kN and 0.062 % at 18 kN. (b) A1=126.68 mm², k1=E1A1/L=173.1 kN/mm, Pgap=k1g≈7 kN. With s≈0.4: F2≈−0.430−7≈−9.2 kN, so the rod carries about 21 kN, σrod≈−164 MPa. (c) Free mismatch 23.6−11.7×10−6×60×100=0.0714 mm. The bolt and sleeve stiffnesses are similar (161 and 157 kN/mm), so each takes about half of the mismatch strain of 714 µε: the bolt strain rises by about 350 µε (exact: 352 µε). Units: K−1 × K × mm = mm.

P2. (a) Appendix D.4 of the handout. (b) A2=221.68 mm², k2=E2A2/L−g=101.9 kN/mm, Pgap=6.925 kN, s=0.3704. F2(10 kN) = −1.139 kN, F2(20 kN) = −4.843 kN, F2(30 kN) = −8.547 kN. Twice F2(10 kN) is −2.278 kN, not −4.843 kN: the first 6.9 kN of every load case goes to the rod alone, so the tube’s force is proportional to P−Pgap, not to P. (c) g→0: F2=−sP, the textbook result. k2→0: F2=0. k2→∞: s→1, F2=−P−Pgap.

P3. (a) Ab=78.54 mm², As=227.57 mm²; L/EbAb+L/EsAs=12.589×10−6 mm/N; dFb/dT=11.9×10−6100/12.589×10−6=94.53 N/K. At 80 °C: Fb=2000+6094.53=7.672 kN; σb=97.7 MPa, σs=−33.7 MPa. (b) Swapped: L/EalAb+L/EstAs gives dFb/dT=−57.70 N/K, so the preload is gone after 2000/−57.70≈34.7 K of heating.

P4. (a) e=βt/6=0.05×6.35/6=0.0529 mm. (b) The front gage reads εx1+β, so Efront=E/1+β: −4.8 % (too low); the back gage gives 5.3 % (too high). (c) εx1+β+εx1−β/2=εx for any β, because the bending strain is linear through the thickness and the gages are symmetric about the mid-plane.

P5. Simulation, presets as shipped: Pgap = 6.925 kN, s = 37.03 %, F2(30 kN) = −8.547 kN; bolt dFb/dT = 94.53 N/K, Fb at ΔT = 60 K = 7.672 kN. These match P2 and P3 exactly. “Superposition fails with a gap” sets P = 20 kN: the tube carries −4.843 kN at 20 kN against −1.139 kN at 10 kN, more than four times as much for twice the load.

P6. (a) The rod yields at F1=370×126.68=46.9 kN. Before contact, F1=−P; after, F1=−Pgap−1−sP−Pgap. Setting F1=46.9 kN gives P≈70.4 kN, 2.35 times the 30 kN limit (the tube is then at 106 MPa, still elastic). (b) Scalding (80 °C water): the hook, gloves, and lifting out only below 40 °C. Electric shock (mains heater and water): GFCI outlet, indicator and leads away from the water. Credit also a wet gage giving false readings (sealed gage; the step-4 check).

## 3. Analysis solutions

A1. b = 25.400 mm, t = 6.350 mm, A = 161.29 mm². Least-squares slope of σ against the average axial strain (loading and unloading, 19 points): E = 68.46 ± 0.93 GPa, intercept −0.002 MPa. Budget (relative u): slope statistics 0.039 %, area 0.21 %, load cell 0.29 %, gage factor 0.58 %. The gage factor dominates. Transverse vs axial slope: ν = 0.330 ± 0.006, intercept −0.17 µε. Agreement (Eq. 21): ΔE = 0.44 ≤ 2.21 GPa; Δν = 0.0004 ≤ 0.021; both agree. G = 25.74 ± 0.37 GPa, close to the handbook 26 GPa. Largest loading–unloading difference 2.2 µε, at the noise level: no yielding or slip. Interpret: a fitted slope uses every point and ignores a zero offset; a ratio of single readings is biased by any offset and has the noise of one reading. To reduce uE, calibrate the gage factor (shunt calibration), not the calipers.

A2. β = 0.0545 (5.45 %), nearly constant above 4 kN, so the offset is geometric: e=βt/6 = 0.0577 mm. Single-gage moduli: front 64.88 GPa (−5.2 %), back 72.45 GPa (5.8 %). Harmonic mean 2/1/Ef+1/Eb = 68.46 GPa, identical to the average-strain E; the arithmetic mean 68.67 GPa is biased high by about β2. Interpret: a one-gage test would have been wrong by about 5 %, 3.8 times the expanded uncertainty (U/E = 1.4 %), with no warning in the data: a perfectly straight σ–ε line can hide a 5 % error.

A3. Areas: rod 126.74 mm², tube 221.82 ± 0.54 mm² (u). Two-parameter fit to the loading branch: Pgap = 6.951 ± 0.051 kN, s = 0.3712 ± 0.0073, residual scatter 16 N. With k1 = 173.2 kN/mm (Table 1 E for steel), g = 0.0401 ± 0.0012 mm. The height gage gives 0.040 ± 0.016 mm; Δ = 0.0001 ≤ 0.0164 mm, agree. The knee is 13 times more precise: it measures the gap through the stiffness of a 150 mm rod, which turns 0.04 mm into 7 kN, while the height gage must resolve the 0.04 mm length difference directly with ±0.01 mm on each length. Theory, Eq. 12 with the measured E and areas: s = 0.3689 ± 0.0076; Δ = 0.0024 ≤ 0.0106, agree. Check: k in N/mm = MPa × mm²/mm. A line forced through the origin (g = 0) misses the data by up to 1.6 kN below 10 kN. Common error: reading Pgap as “the first load where the tube strain is non-zero” (8 kN), which overstates g by 15 %.

A4. At 30 kN: tube −8.527 kN (measured), rod by equilibrium −21.49 kN; stresses −169.5 MPa (rod) and −38.4 MPa (tube), both well below yield. Eq. 11 with the fitted Pgap and s: −8.561 kN (0.40 % from the measurement). The textbook no-gap result −sP = −11.070 kN overstates the tube force by 29.8 %. Apparent share F2/−P: 8 kN: 0.047, 12 kN: 0.156, 20 kN: 0.243, 30 kN: 0.284; theory at 30 kN s1−Pgap/P = 0.285. It approaches s only as P→∞. Check: the unloading branch gives s = 0.3707, the same line as loading; tube gages differ by 3.1 % (bending), removed by averaging. Interpret: for the no-gap formula to be within 5 % at 30 kN, Pgap/P−Pgap≤0.05, so Pgap≤ 1.43 kN and g≤ 8.2 µm: a tolerance tighter than ordinary machining. Fit-up controls load sharing in short, stiff assemblies.

A5. Below the knee (2–6 kN): slope 7.77 ± 0.14 µm/kN (u); 1/k1 = 5.77 µm/kN, so C = 1.99 ± 0.16 µm/kN. Above the knee: slope 5.083 ± 0.021 µm/kN; 1/k1+k2 = 3.64 µm/kN, so C = 1.44 ± 0.04 µm/kN. The two estimates differ by 3.3 combined standard uncertainties: they disagree. Cause: the low-load points include the seating of the caps and the dial (a toe, as in Lab 1), which adds apparent compliance between 2 and 6 kN. The above-knee estimate is the reliable one (true value 1.50 µm/kN). Check: units µm/kN = mm/MN. Interpret: the dial reads members, caps and seating in series, and C is about 28 % of the post-contact slope, so it cannot isolate the members. The gages measure the tube’s own strain, independent of C.

A6. Ab = 78.59 mm², As = 227.62 mm². Preload at 20 °C: 124.0 µε → 1.998 kN. Fit of Fb against T (all 19 points): slope 6.060 ± 0.059 µε/K → dFb/dT = 97.6 ± 9.9 N/K (relative u 5.0 %, dominated by the residual-thermal-output allowance, 4.8 %). Heating alone 97.5, cooling alone 97.9 N/K: no slip. Prediction, Eq. 16, with Es from A1: flexibility sum 12.6242 × 10−6 mm/N, 94.3 ± 6.9 N/K (dominated by the uncertainty in αs−αb). Δ = 3.4 ≤ 12.0 N/K: agree. At 80 °C: Fb = 7.856 kN, σb = 100.0 MPa, σs = −34.5 MPa. Two effects: (1) residual thermal output: ±0.5 µε/K × EbAb = ±8.1 N/K, either sign; the truth model’s +0.4 µε/K adds +6.4 N/K. (2) The sleeve’s modulus falls 1.8 % over 60 K, which changes the average slope by −1.2 % (from 94.3 to 93.1 N/K). The measured excess of 3.4 N/K is consistent with a small positive residual output; the modulus effect alone would push the slope the other way. Check: Fb>0 throughout, so the joint never separated.

A7. Table K1 supplies the entries; simulation values are in P5. Expected verdicts: E, ν, Pgap (vs. Eq. 10 with the height-gage g, whose large U makes agreement easy), s and dFb/dT all agree; F2 at 30 kN agrees with Eq. 11 but not with the no-gap formula. The normalized plot should show the knee-based Pgap with a much smaller error bar than the height-gage prediction. Full credit requires students to state that the agreement for Pgap is weak evidence, because the reference is imprecise.

M1. (a) Measured F2(20 kN)/F2(10 kN) = −4.852/−1.131 = 4.29, not 2. Superposition requires a linear system with a fixed set of active constraints; the tube’s contact is a one-sided constraint that switches on at Pgap, so the response is only piecewise linear. (b) The rod yields before the tube engages if k1g>σYA1, i.e. g>σYL/E1 = 370 × 150/205 000 = 0.271 mm. In “Gap never closes” (g = 0.4 mm), Pgap = 69.3 kN while the rod is already at 474 MPa at 60 kN, and the yield warning shows. With g = 0.27 mm and P just above Pgap, the warning appears as the tube engages. (c) Aluminum bolt in steel sleeve: dFb/dT = −57.70 N/K, so ΔTsep = 2000/−57.70 ≈ 34.7 K. At 120 K the bonded formula gives Fb = −4.92 kN (a bolt in compression), which is impossible: the head lifts off the sleeve, the joint is loose, and both forces are zero. Eq. 16 assumed the members stay in contact.

## 4. Challenge and Extension solutions

C1. “Refine a taper” (aluminum cone 30 → 15 mm over 400 mm plus a 100 mm segment of 15 mm diameter, fixed at both ends, heated 60 K; R = 28.734 kN). Relative error in R: N = 1: 8.00e-02; N = 2: 2.28e-02; N = 4: 5.97e-03; N = 8: 1.51e-03; N = 16: 3.79e-04; N = 32: 9.49e-05; N = 64: 2.37e-05; N = 128: 5.93e-06. Log–log slope 1.970 (theory 2). The finite element with the midpoint area integrates ∫dx/A by the midpoint rule, whose error per element is h3/241/A″, summing to Oh2 over the length. On a prismatic segment 1/A is constant, the midpoint rule is exact, and so is the element for any N.

C2. From Eq. 16: αs=αb+dFb/dTfb+fs/L = 24.02 ± 1.40 × 10−6/K. Handbook 23.6; Δ = 0.42 ≤ 1.52 × 10−6/K: agree. The dominant term is udFb/dT, itself dominated by the gage’s residual thermal output. The truth model used 23.4 × 10−6/K: this measurement is 2.7 % high, consistent with the +0.4 µε/K residual.

C3. At 18 kN: εx = 1 631 µε, εy=εz = −538 µε. Width change −13.7 µm, thickness change −3.4 µm. Dilatation 1−2νεx = 556 × 10−6. The caliper’s u is about 12 µm, so the width change is about one standard uncertainty: not measurable. Bulk modulus E/31−2ν = 67.0 GPa. ν=0.5 means zero volume change (incompressible, infinite bulk modulus): the limit approached in plastic flow (Lab 1’s constant-volume assumption), not in elastic metals.

X1. EαΔTA=4π2EI/L2 with I/A=d2/16 gives ΔTcr=π2d2/4αL2; E cancels. Example: 10 mm × 0.5 m steel bar, 84.4 K. Yield occurs at ΔTY=σY/Eα = 154 K. Buckling comes first when π2d2/4αL2<σY/Eα, i.e. L/d>π/2E/σY = 37.0 for 1018 steel. The simulation experiment (8 mm and 6 mm segments, 1.2 m long, heated 120 K) reports a compressive force of 6.94 kN against a fixed–fixed Euler load of 0.120 kN for the thinnest section; by the formula above, that bar buckles after about 2.61 K.

X2. With Es falling 0.03 %/K, Eq. 16 predicts a quadratic coefficient of about −0.0146 N/K² and a largest departure from a straight line of 8.6 N (0.54 µε) over 60 K. The quadratic fit to the data gives −0.022 ± 0.029 N/K² (u): the standard error is about twice the predicted effect, so it is not detectable. A larger range (to 150 °C in oil), averaging several readings per step, or a full-bridge bolt gage (2.6 times the signal) would be needed. The effect on the mean slope, −1.2 %, is also well below u.

X3. Brass tube A3 = 231.7 mm², k3 = 149.8 kN/mm, shorter than the rod by g + 0.040 mm. Events: aluminum tube engages at 6.95 kN; brass tube engages when the caps have moved a further 0.040 mm, at 17.93 kN (P=P1+0.040k1+k2). At 30 kN: rod −18.81 kN, aluminum tube −6.93 kN, brass tube −4.26 kN (sum −30.000 kN = −P). Grade the program on event detection (sorted gaps, or a check on each member’s contact at each step) and on the equilibrium check.

## 5. Design problem D1: reference solution

D1. αL = 0.0708 mm/K for a 3.00 m segment. Hot requirement (worst case: installed at the coldest, 10 °C; hottest service, 55 °C): free growth α55−10L = 3.186 mm. The allowed restrained shortening is σallowL/E = 40 × 3000/68 459 = 1.753 mm, so g≥ 3.186 − 1.753 = 1.43 mm. (With g = 0 and installation at 15 °C the stress would reach 64.6 MPa.) Cold requirement (worst case: installed at 20 °C; −25 °C service): the gap grows by 3.186 mm, so g≤ 8.0 − 3.186 = 4.81 mm.

Design 1 (fixed gap): g = 3.12 ± 1.69 mm satisfies both requirements for any installation temperature in 10–20 °C. A specification of 3.0 ± 1.0 mm is easy for a crew to hold with feeler gages and leaves margins of about 0.6 mm and 0.8 mm on the two bounds. Design 2 (temperature rule): set gTinst=3.12−0.0708Tinst−15 °C mm, which keeps the full band width of 4.09 mm (tolerance ±2.04 mm) at any installation temperature: more tolerance, at the cost of measuring the rail temperature at installation. Uncertainty: Uα moves each bound by ±0.081 mm; UE moves the hot bound by ±0.024 mm. Both are small compared with the band. A robust answer shrinks the band by these amounts. Assumptions that could invalidate the design: the rail’s temperature in sun can exceed the air temperature by 20–30 K (check with a contact thermometer on a summer day); the posts are not rigid, so restrained stress is overestimated (conservative); buckling between posts governs the 40 MPa limit (check with Lab 9’s Euler formula for the post spacing).

Rubric detail (15 points total in the report). Requirements (3): both translated, including that the hot case allows closure plus restrained stress. Worst cases (3.75): opposite installation-temperature extremes for the two requirements. E and α (2.25): uses measured E; mentions Uα. Specification and trade-off (4.5): a nominal value and a tolerance, or a rule, checked against both bounds, compared with an alternative. Presentation and assumption (1.5). Typical partial credit: using 15 °C for both bounds (−3); requiring g≥ the full free expansion, ignoring the allowed stress (−2, the design still works but is over-constrained); using the textbook E instead of the measured one (−1).

## 6. Expected ranges for real class data

Table K2. Expected data ranges.

| Quantity | Expected | If outside, suspect |
| --- | --- | --- |
| E of 6061-T6 from Part A (GPa) | 66–71 | gage factor setting, single-gage use, area from nominal |
| ν | 0.31–0.35 | transverse gage misaligned; ratio of single readings |
| β in Part A | below 0.10 | grips not seated; re-grip |
| Gap from the knee (mm) | as machined, typically 0.02–0.08 | caps not flat; rod or tube ends not square |
| s after contact | 0.35–0.39 | wrong tube area (gross instead of annulus); E of steel used for the tube |
| C above the knee (µm/kN) | 1–4 | fit range includes the knee or the toe |
| dFb/dT (N/K) | 85–105 | uncompensated gage (reads total strain: about 6 times too large); temperature not settled |
| Preload (kN) | 1.9–2.1 | gage not zeroed with the nut finger-tight |

## 7. Common student mistakes

- Using one gage of a pair, or averaging the two single-gage moduli instead of the strains.

- Taking ν as −εy/εx at one load instead of fitting a slope.

- Writing equilibrium as F1+F2=P with tension-positive member forces, which gives tension in a squeezed assembly.

- Computing the share as F2/P at the largest load (A4) and calling it s.

- Using the outer-diameter area for the tube, or the steel modulus for the aluminum tube.

- Picking Pgap as the first non-zero tube reading instead of fitting the knee.

- Subtracting αbΔT from the compensated bolt gage, which the gage has already done.

- Measuring ΔT from 0 °C instead of from the preload temperature.

- Adding stiffnesses instead of flexibilities in the denominator of Eq. 16 (members in series around the loop of the joint).

- In D1, using one installation temperature for both requirements, or ignoring that the hot case allows the gap to close.

- Mixing µε and mε, or α per °F and per K.

## 8. Grading rubric

Table K3. Grading rubric (100 points plus up to 10 Challenge points).

| Part | Points | Full credit | Common deductions |
| --- | --- | --- | --- |
| Pre-lab | 15 | P1–P6 correct with units; P1 an estimate made before measuring | P2 without the superposition explanation (−2); P2(c) limits missing (−1) |
| Data & procedure | 10 | Tables 3–6 complete; checks in steps 2, 4, 8 and 12 recorded | Part C readings before the temperature settled (−3) |
| A1 | 8 | E, ν, G with budgets and agreement tests | no budget (−3); ratio instead of slope for ν (−2) |
| A2 | 5 | β, e, single-gage moduli, harmonic-mean check | arithmetic mean claimed equal (−1) |
| A3 | 8 | two-parameter fit, g with U, comparison with height gage, s vs. Eq. 12 | knee by eye (−3) |
| A4 | 7 | stresses, Eq. 11 vs. no-gap comparison, apparent share, tolerance | no tolerance answer (−2) |
| A5 | 5 | both C estimates, disagreement found and explained | disagreement not noticed (−2) |
| A6 | 8 | slope, preload, prediction with U, stresses, two effects quantified | uncompensated-strain error (−4) |
| A7 | 4 | complete table, normalized error-bar figure, every discrepancy explained | unexplained discrepancy (−1 each) |
| M1 | 10 | ratio from data; gcrit derived and checked; separation temperature and why Eq. 16 fails | no simulation confirmation (−2 each) |
| D1 | 15 | see Sec. 5 | see Sec. 5 |
| Communication | 5 | labeled axes, units, x±U format | each unlabeled axis (−1) |
| Challenge | +10 | C1 (4), C2 (3), C3 (3) | — |

Every Core answer must include the required check and interpretation; deduct 1 point per question where either is missing.

## 9. Instructor notes

Before the lab. Part A: a 300 mm 6061-T6 flat bar with a 0°/90° gage pair (axial and transverse) on each wide face at mid-length. Part B: face the rod and the tube in the same lathe setup so that the tube ends up 0.03–0.06 mm shorter and both ends are square; harden or use tool-steel caps at least 40 mm thick so that C stays small; bond two axial gages on opposite sides of the tube at mid-length (75 mm from each end, more than ten wall thicknesses from the caps). Part C: bond a steel-compensated (STC 06) gage on the bolt shank, coat it for immersion (nitrile or polysulfide coating), run the leads along the shank and out through a 2 mm notch at the nut end of the sleeve, and test it in warm water the day before. Check the bath’s GFCI.

Timing (2 h). 0:00–0:10 safety briefing, collect P1–P6; 0:10–0:20 Part C preload and into the bath, heater on; 0:20–0:50 Part A while one partner records Part C every 5 °C; 0:50–1:25 Part B; 1:25–1:45 Part C cooling readings and dimensions; 1:45–2:00 simulation (step 13). With more than four teams, run Part C as one shared station with a single bath and post its readings for everyone.

Safety. Demonstrate the hook and the lift-out before anyone heats water. Never let a team open the shield during Part B loading: a cap that is not centred can eject the stack sideways at 30 kN. The 30 kN limit leaves a factor of 2.35 on rod yield.

Running without equipment. Give students sample_data.csv and Appendix A of the handout; everything in this key applies unchanged. A good hybrid is to run Part B live (the knee is striking to watch) and use the sample data for Parts A and C.

Your own class data. Export each part in the column layout of Table A1, fill a measurements JSON like src/specimen_measurements.json (including the height-gage lengths), and run src/lab02_analysis.py and src/make_key.py.

The simulation. Students use it in P5, step 13, A7, M1, C1 and X1. Its readout shows closed form vs. numerical agreement for every quantity; the Node and Python tests in tests/ and the record in tests/VERIFICATION.md show that the two agree to round-off for prismatic members and converge as N−2 for the taper.

## 10. Self-critique and revisions

Before release, the lab was reviewed as a demanding instructor at a top program would review it. The three biggest weaknesses found, and the fixes made:

- The gap in Part B was going to be read off the first non-zero tube reading. With 2 kN steps this locates Pgap only to ±1 kN (15 % of its value), so the comparison with theory was meaningless. Fix: the handout now fits the two-parameter model of Eq. 11 by least squares (Appendix D.7), and A3 asks for the gap with its uncertainty and a comparison with an independent height-gage measurement. The fit is 13 times more precise than the height gage.

- An ordinary gage on the bolt would read total strain, about αbΔT = 700 µε of free expansion on top of the 350 µε mechanical signal. Students would have had to subtract a large, uncertain number. Fix: Part C specifies a gage compensated for steel, the handout explains what it reads (Sec. 2.4), Table 2 states its residual thermal output, the uncertainty budget includes it, and A6 asks students to quantify its effect against the modulus drift.

- Three experiments did not fit in two hours, mainly because heating a bath takes 30–45 minutes with settling time at each step. Fix: the procedure starts Part C first and runs Parts A and B on the machine while it heats, and the instructor notes give a minute-by-minute plan and a shared-station option for large sections.

Known limitations (not fixed). The simulation treats the caps as rigid (C = 0) and the moduli as independent of temperature; A5 and X2 address both from the data. The sample data have no temperature lag between bath and bolt, so heating and cooling slopes agree better than a live test will show. Saint-Venant end zones at the caps are outside the 1-D model; the gages are placed far enough away (75 mm, more than ten wall thicknesses) that this does not matter here.